## Slide 1: Electropolymerization of Aniline
Nikolas Vitaliti s223455

## Slide 2
Conducting polymer - Polyaniline
Redox states of PANI
  Leucoemerladine - poor conductor, fully reduced
  Emeraldine - great conductor (delocalized polaron), intermediate
  Pernigraniline - poor conductor, fully oxidised

## Slide 3
Electrodepositon
Potentiodynamic
CV characterization
Potentiostatic
CV characterization
UV – vis absorption spectroscopy
Over oxidation
Methodology

## Slide 4: Experimental setup
Three electrode setup
WE: Transparent conducting flourine doped tin oxide electrode (FTO)
CE: Coiled platinum wire
RE: Ag/AgCl with 1M KCl filling solution
Electrolytes
  Electrodepositon: H2SO4 + aniline
  Characterization: H2SO4

## Slide 5: Synthesize of polyaniline
Anodic oxidation of Aniline in aqueous sulfuric acid solution
Aniline oxidizes at the negatively charge anode
Radical formation after oxidation
Polymer forms at the WE

## Slide 6
Electrodeposition of aniline
Film 1
Electrodynamically deposited through CV at 50 mV/s
Peak current increases with the number of cycles
Film 2
Electrostatically deposited through CA
Voltage fixed at:
  0.75V for oxidation (300 s)
  -0.3V for reduction (30 s)
Notes: Add aniline to polyaniline, 0.8 gives polyaniline

## Slide 7: Film comparison
Film 2: potentiostatic
Film | Oxidation charge [C] | Reduction charge [C]
1 | 0.0143 | 0.0111
2 | 0.0411 | 0.0382
Film 1: potentiodynamic
Film | State | Mass [µg] | Thickness [nm] | Γ [10-8 mol/cm2]
1 | Oxidation | 6.88 | 43.1 | 6.15
 | Reduction | 5.34 | 33.4 | 4.78
2 | Oxidation | 19.8 | 124 | 17.7
 | Reduction | 18.4 | 116 | 16.5
3 cycles 50 mV/s between −0.3V and 1.0V vs Ag/AgCl

## Slide 8: Scan rate dependence
For surface confined and fully reversible species peak current is directly proportional to the scan rate:
Linear relation between peak current and scan rate
R2 = 0.996
R2 = 0.997

## Slide 9: Redox states
CV at 50 mV/s to fully oxidize and fully reduce
Unexpected peak:
ortho-coupled polymers
degradation of PANI
Notes: Rinsing of WE revealed vague colour change in droplet – shorter oligomers are soluble
Possibly due to degradation of PANI and formation of species like benzo- and hydroquinone

## Slide 10: UV-vis spectroscopy
Absorption at potential holds corresponding to different redox states
Two absorption ranges:
Oxidation leads to:
  Darker film
  Higher absorption in the 300-400 nm range
After 600 nm peaks at different wavelength for different redox states
  300 - 400 nm​
  600 - 900 nm

## Slide 11: PANI at higher potentials
Absorption after CV at higher potentials and potential hold at 0.35 V
Less absorbance after over-oxidation
Decreasing current
Emeraldine

## Slide 12: Conclusion
PANI is an interesting polymer to investigate as it’s easily tunable between its different redox states:
  Leucoemerladine
  Emeraldine
  Pernigraniline
Observed a linear relation between peak current and scan rate
Absorption in two ranges (300-400 nm and 600-900 nm)
Overoxidation lead to degradation of polyaniline

## Slide 13
Thank you!