## Slide 1: Organic Redox (Flow) Battery
Nikolas Vitaliti s223455

## Slide 2: Introduction
ARS (Alzarine Red s)
Ferrocyanide
Investigate the properties of an organic redox (flow) battery
Ferrocyanide as posolyte and ARS as negolyte
Electrode reactions:
Notes: ARS: two-electrode response

## Slide 3: Flow chart
Cyclic Voltammetry
Charge - Discharge
SOC
Volumetric capacity
Volumetric energy density
Cell potential
Electrolytes
Battery
Methodology

## Slide 4: Experimental setup
WE: Glassy carbon disk coated in a chemically resistant polymer
CE: Coiled platinum wire
RE: Ag/AgCl
CYCLIC VOLTAMMETRY
Three electrode setup
Aqueous solution of 1 M KOH:
  2 mM Ferrocyanide​
  2 mM Alzarine Red s (ARS)
Aqueous solution of 1 M KOH :
  Posolyte: 1.8 mL of 0.2 M Ferrocyanide​
  Negolyte: 2.3 mL of 0.05 M ARS
CHARGE-DISCHARGE EXPERIMENT

## Slide 5: Cyclic Voltammetry
 | ARS | Ferrocyanide
Epa | -0.9 V | 0.35 V
Epc | -0.94 V | 0.17 V
Investigate redox potential
Assumption: equal diffusion (i.e. capacity-balanced cell)
E0'pos = 0.26 V E0'neg = - 0.92 V
scan rate: 50 mV/s

## Slide 6: Charge-Discharge
Full cycle took 23.3 min
Loss of capacity

## Slide 7: Charge-Discharge
Increasing time i.e. lower C-rate:
Expect stationary CE and increased VE
However, a open-to-atmosphere-cell leads to side reactions
Relatively good!
Notes: CE= how much charge is in the battery versus how much charge do we actually put in
VE= Voltage efficiency measures the effects of cell polarisation or cell voltage losses.
EE= energy output with respect to our input

## Slide 8: State of Charge
Theoretical overall cell potential as function of SOC:
Using the redox potential values :
This should be compared to the experimental SOC for charge and discharge:
E0'pos = 0.26 V
E0'neg = - 0.92 V
*p and q being initial molarities of oxidized and reduced posolyte (i.e. limiting agent)
*

## Slide 9: Volumetric Energy Density
Volumetric capacity of the investigated flow batttery
Energy density of investigated battery
Energy density of a capacity-balanced battery
Same effective concentration
Maximum solubility of ARS in 1 M KOH is 0.55 M (earlier 0.05 M)
Same cell potential as the experimental battery
Q
Experimental battery
Capacity-balanced battery

## Slide 10: Conclusions
Redox potentials estimate to be 0.26 V for Ferrocyanide and –0.92 V for ARS
Overall good efficiencies: CE= 91.9% , VE= 80.3% , EE= 73.8%
Slower C-rates generally increase VE and therefore ultimately increase EE
Polarization leads to high losses in the charging-discharging process
Assuming a capacity balanced battery greatly increases energy density
Even by using the maximum solubility of ARS in 1M of KOH the energy density is still low
Notes: Using the maximum solubility of ARS

## Slide 11
Thank you!